8D REPORT — OEM Norte Supplier Quality

Form OEMN-SQ-8D rev. 3 · to be returned within 10 working days

| Supplier | Componentes Arga S.L. | Supplier code | ARGA |
| --- | --- | --- | --- |
| OEM Norte complaint no. | C-OEMN-2024-0128 | Supplier 8D no. | 8D-ARGA-2024-004 |
| Part number | AR-1003 | Part description | Battery tray bracket LH |
| Special characteristic | MIG weld strength (CC) | Supplier lot | L24094-AR1003-01 |
| Complaint date | 2024-05-14 | Qty complained | 38 |
| Containment due (24 h) | 2024-05-15 | 8D due (10 WD) | 2024-05-28 |
| Report status | CLOSED | Closure date | 2024-08-26 |

# D1 · Team

| Name | Role | Department |
| --- | --- | --- |
| Iñaki Etxeberria | Quality Manager (champion) | Quality |
| Maialen Irigoyen | Customer Quality Engineer (8D leader) | Quality |
| Oihana Zabaleta | Welding Process Engineer | Engineering L2 |
| Xabier Urrutia | Production Manager L2 | Production |
| Ander Goñi | Night Shift Leader L2 | Production |
| Mikel Aranburu | Metrology & Lab Technician | Quality |
| Koldo Arbizu | Maintenance Manager | Maintenance |

Customer contact: M. Ruiz, Supplier Quality Engineer, OEM Norte battery module assembly.

# D2 · Problem description (5W2H)

Problem statement

OEM Norte reported 38 battery tray brackets LH (AR-1003) with a crack along MIG weld seam W2 (bracket-to-gusset fillet weld, 45 mm long). The parts failed the pull-out test at the battery tray sub-assembly station (requirement ≥ 18 kN); cracked parts broke between 9 and 12 kN. All complained parts are traceable to lot L24094-AR1003-01.

| 5W2H |  |
| --- | --- |
| What | Crack / lack of fusion at the root of seam W2 (fillet a = 3.0 mm). Characteristic 'MIG weld strength' is classified CC. |
| Where | Detected at OEM Norte, pull-out test station of the battery tray sub-assembly. Origin: Arga L2, robot cell CR-01, program P12. |
| When | Lot produced 03/04/2024 on the night shift, delivered 09–10/04/2024, detected by the customer on 13/05/2024. |
| Who | Detected by an OEM Norte line operator; reported by the OEM Norte SQE. |
| Which | AR-1003 only. AR-1004 (RH, same cell and wire) was checked at the customer: no failures. |
| How | Fracture along the weld root; macro-section shows root penetration of 0.4–0.6 mm (requirement ≥ 1.0 mm). |
| How many | 38 parts NOK out of 1,189 delivered from the lot (3.2 %). |

Lot L24094-AR1003-01: produced 2024-04-03 (night shift), press PR-400, cell CR-01, 1,200 parts produced, 11 scrapped. Steel coil S-ULTZ-240183, MIG wire S-GOIE-240126, e-coat chemistry S-ARAK-240127.

# D3 · Interim containment actions

Containment started on 2024-05-14, within 24 h of notification. Scope: every AR-1003 lot welded on CR-01 from the complained lot up to the notification date (ERP lots, delivery notes and finished-goods stock).

| Lot | Part | Prod. date | Shift | Qty OK produced | Shipped (delivery notes) | Arga stock | Action | Result |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| L24094-AR1003-01 | AR-1003 | 2024-04-03 | night | 1,189 | 1,189 (AL-24-00185, AL-24-00186) | 0 | Sorting at customer | 41 NOK |
| L24101-AR1003-01 | AR-1003 | 2024-04-10 | afternoon | 1,988 | 1,988 (AL-24-00201, AL-24-00202) | 0 | Sorting at customer | 0 NOK |
| L24108-AR1003-01 | AR-1003 | 2024-04-17 | night | 2,266 | 2,266 (AL-24-00216) | 0 | Sorting at customer | 3 NOK |
| L24115-AR1003-01 | AR-1003 | 2024-04-24 | morning | 884 | 884 (AL-24-00230, AL-24-00231) | 0 | Sorting at customer | 0 NOK |
| L24122-AR1003-01 | AR-1003 | 2024-05-01 | afternoon | 2,746 | 2,746 (AL-24-00247) | 0 | Sorting at customer | 0 NOK |
| L24129-AR1003-01 | AR-1003 | 2024-05-08 | night | 1,688 | 844 (AL-24-00262) | 844 | Blocked + 100 % sorting | 0 NOK |

Finished-goods stock at Arga (844 parts) blocked in the ERP on 2024-05-14 and 100 % re-inspected: visual inspection of seam W2 with 10x loupe + chisel test 1 part in 50.

Customer stock and parts in transit sorted by the Arga resident team at OEM Norte on 2024-05-15–2024-05-17 (visual + dye penetrant on seam W2).

Destructive pull-out test, 5 parts per suspect lot: all ≥ 21 kN except lot L24094-AR1003-01 (2 of 5 below 18 kN).

Certified parts identified with a green dot label 'CP 8D-ARGA-2024-004' until the effectiveness check is closed.

# D4 · Root cause analysis

Root cause workshop on 2024-05-18 (Ishikawa + 5 Whys) with the three L2 shift leaders; weld trials on 2024-05-19.

Ishikawa diagram (6M)

| Category | Potential cause | Verification / status |
| --- | --- | --- |
| Man | Operator adjusted welding parameters on the teach pendant without authorisation | CONFIRMED – wire feed speed override −8 % found active on P12 |
| Machine | Wire feeder / drive rolls of CR-01 | Ruled out – feed speed stable within ±1 % (measured 16/05/2024) |
| Machine | Contact tip and gas nozzle wear | Ruled out – spatter build-up observed, tip replaced on 16/05/2024; trial welds with the removed tip at nominal parameters passed macro-section (n = 3) |
| Method | No start-of-shift verification of welding parameters in IT-L2-CR01-03 v1 | CONFIRMED |
| Material | MIG wire lot S-GOIE-240126 (G3Si1 Ø1.0 mm), in use since 20/03/2024 | Ruled out – 3.1 certificate conform, Si/Mn within specification |
| Material | Steel coil S-ULTZ-240183 (HSLA 420, 3.0 mm) | Ruled out – certificate conform, CEV 0.38 |
| Measurement | In-process weld check: visual + chisel test 1 part per shift | CONFIRMED (non-detection) – cannot reveal root lack of fusion |
| Environment | Shielding gas flow M21 (Ar 82 / CO2 18) | Ruled out – 15 l/min measured at the nozzle |

5 Whys — occurrence

| Why |  |
| --- | --- |
| 1 | Why did seam W2 crack in the pull-out test? — Insufficient root penetration (0.4–0.6 mm). |
| 2 | Why was penetration insufficient? — Heat input about 15 % below the window qualified in WPS-CR01-03. |
| 3 | Why was heat input low? — Wire feed speed override of −8 % (8.6 m/min vs 9.4 ± 0.3 m/min) and arc voltage at the lower limit on program P12. |
| 4 | Why was the override active? — It was set on the teach pendant during the night shift of 03/04/2024 to reduce spatter and was neither reset nor recorded. |
| 5 | Why was this possible? — Parameter screens were not password-protected and IT-L2-CR01-03 v1 did not require a start-of-shift parameter check. |

5 Whys — non-detection

| Why |  |
| --- | --- |
| 1 | Why was the defect not detected at Arga? — Visual inspection and the chisel test (1 part/shift) do not reveal lack of fusion at the root. |
| 2 | Why is there no more sensitive test? — Macro-sections were only required for PPAP and requalification, not in series production. |
| 3 | Why? — The PFMEA rated detection D = 4 assuming the chisel test was effective; its effectiveness had not been validated. |

Root cause — occurrence: Welding parameters of program P12 on CR-01 were outside the WPS window (wire feed speed override −8 % set manually and not reset), resulting in insufficient heat input and lack of fusion at the root of seam W2.

Root cause — non-detection: The control plan relied on visual inspection and a chisel test once per shift, which cannot detect root lack of fusion; no periodic macro-section or pull-out test at Arga.

Root cause verification: Defect reproduced on 2024-05-19: 10 parts welded with WFS −8 % → 4/10 below 18 kN, penetration 0.5 mm. 10 parts at nominal parameters → 10/10 ≥ 22 kN, penetration 1.3–1.6 mm.

# D5 · Permanent corrective actions (chosen)

| Action | Type | Owner | Due date |
| --- | --- | --- | --- |
| Password protection of welding parameters on the CR-01 and CR-02 teach pendants (level 2 = process engineer) | Corrective – occurrence | Koldo Arbizu | 2024-05-23 |
| Start-of-shift parameter check (WFS, voltage, gas flow) recorded on the cell checklist, included in IT-L2-CR01-03 v2 | Corrective – occurrence | Oihana Zabaleta | 2024-05-26 |
| Macro-section 1 part per week and per program + chisel test 1 part per shift | Corrective – detection | Mikel Aranburu | 2024-05-26 |
| Pull-out test at Arga lab, 3 parts per lot (≥ 18 kN) | Corrective – detection | Mikel Aranburu | 2024-05-28 |

# D6 · Implementation and validation

Actions implemented between 2024-05-24 and 2024-06-03. Parameter lock active since 2024-05-24. IT-L2-CR01-03 v2 released on 2024-05-28 with the start-of-shift checklist; operators of the three shifts trained (attendance sheet TR-L2-2024-019). Macro-section and lot pull-out test added to PC-AR1003-01 v2.

Validation results

Pull-out tests weeks 21–29/2024: 42 lots × 3 parts, minimum 20.4 kN, Cpk 1.71.

Macro-sections: 12/12 with root penetration ≥ 1.1 mm.

No further complaints from OEM Norte on AR-1003/AR-1004 in the 90 days after implementation.

# D7 · Actions to prevent recurrence

| Action | Document / system | Owner | Due date | Status |
| --- | --- | --- | --- | --- |
| PFMEA: new cause 'parameter change on the pendant', O 5→3, D 6→4 | AMFE-AR1003-01 v2 | Oihana Zabaleta | 2024-06-13 | Done |
| Control plan: macro-section and lot pull-out test | PC-AR1003-01 v2 | Maialen Irigoyen | 2024-06-13 | Done |
| Read-across: parameter lock on CR-02 programs (AR-1005, AR-1009, AR-1010) | CR-02 robot controller | Koldo Arbizu | 2024-06-18 | Done |
| Lessons learned presented at the monthly quality meeting | LL-2024-06 | Maialen Irigoyen | 2024-06-23 | Done |

# D8 · Closure and team recognition

8D closed on 2024-08-26 after the 90-day effectiveness check; closure accepted by the OEM Norte SQE. Management thanked the team at the monthly quality review.

| Role | Name | Date | Signature |
| --- | --- | --- | --- |
| Customer Quality Engineer (8D leader) | Maialen Irigoyen | 2024-08-26 | signed |
| Quality Manager (champion) | Iñaki Etxeberria | 2024-08-26 | signed |
| OEM Norte SQE (acceptance) | M. Ruiz | 2024-08-29 | accepted |