8D REPORT — OEM Norte Supplier Quality

Form OEMN-SQ-8D rev. 3 · to be returned within 10 working days

| Supplier | Componentes Arga S.L. | Supplier code | ARGA |
| --- | --- | --- | --- |
| OEM Norte complaint no. | C-OEMN-2024-0163 | Supplier 8D no. | 8D-ARGA-2024-009 |
| Part number | AR-1009 | Part description | Low-temperature radiator bracket |
| Special characteristic | E-coat thickness (SC) | Supplier lot | L24151-AR1009-01 |
| Complaint date | 2024-07-09 | Qty complained | 260 |
| Containment due (24 h) | 2024-07-10 | 8D due (10 WD) | 2024-07-23 |
| Report status | CLOSED | Closure date | 2024-10-01 |

# D1 · Team

| Name | Role | Department |
| --- | --- | --- |
| Iñaki Etxeberria | Quality Manager (champion) | Quality |
| Maialen Irigoyen | Customer Quality Engineer (8D leader) | Quality |
| Garazi Lizarraga | Process Engineer L3 (e-coat) | Engineering L3 |
| Leire Sarasola | Supplier Quality Engineer | Purchasing |
| Mikel Aranburu | Metrology & Lab Technician | Quality |

Customer contact: M. Ruiz, Supplier Quality Engineer, OEM Norte.

# D2 · Problem description (5W2H)

Problem statement

OEM Norte reported pores and craters in the e-coat of 260 low-temperature radiator brackets (AR-1009) and red rust after 240 h in the neutral salt spray test (requirement: no red rust at 480 h). Lot L24151-AR1009-01.

| 5W2H |  |
| --- | --- |
| What | Pinholes and craters Ø0.2–0.8 mm, mainly on the flat face; e-coat thickness 14–17 µm locally (spec 18–25 µm). |
| Where | Detected at OEM Norte incoming audit and confirmed in their lab. Origin: Arga L3, e-coat line EC-01. |
| When | Lot produced 30/05/2024 (night shift), e-coated on 31/05/2024, delivered 05 and 07/06/2024. |
| Who | OEM Norte incoming quality lab. |
| Which | AR-1009 lots coated with bath make-up chemistry lot S-ARAK-240132. |
| How | Craters with contamination at the centre (EDX: phosphorus and zinc). |
| How many | 260 NOK reported out of 1,393 delivered. |

Lot L24151-AR1009-01: produced 2024-05-30 (night shift), press PR-250, cell CR-02, 1,400 parts produced, 7 scrapped. Steel coil S-ULTZ-240131, MIG wire S-GOIE-240128, e-coat chemistry S-ARAK-240132.

# D3 · Interim containment actions

Containment launched on 2024-07-09. Scope: all AR-1009 lots e-coated since the complained lot until the notification date.

| Lot | Part | Prod. date | Shift | Qty OK produced | Shipped (delivery notes) | Arga stock | Action | Result |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| L24151-AR1009-01 | AR-1009 | 2024-05-30 | night | 1,393 | 1,393 (AL-24-00312, AL-24-00313) | 0 | Sorting at customer | 290 NOK |
| L24158-AR1009-01 | AR-1009 | 2024-06-06 | morning | 1,781 | 1,781 (AL-24-00327, AL-24-00328) | 0 | Sorting at customer | 34 NOK |
| L24165-AR1009-01 | AR-1009 | 2024-06-13 | afternoon | 995 | 995 (AL-24-00342) | 0 | Sorting at customer | 21 NOK |
| L24172-AR1009-01 | AR-1009 | 2024-06-20 | night | 1,179 | 1,179 (AL-24-00358) | 0 | Sorting at customer | 9 NOK |
| L24179-AR1009-01 | AR-1009 | 2024-06-27 | morning | 1,177 | 1,177 (AL-24-00372) | 0 | Sorting at customer | 0 NOK |
| L24186-AR1009-01 | AR-1009 | 2024-07-04 | afternoon | 1,787 | 1,787 (AL-24-00387) | 0 | Sorting at customer | 0 NOK |

Arga stock (0 parts) blocked on 2024-07-09; 100 % visual inspection under 1,000 lux + thickness check (5 points per part, 1 part in 20).

Parts at OEM Norte sorted by the Arga resident team on 2024-07-10–2024-07-11; NOK parts returned for re-coating and scrapped (re-coat not approved by the customer).

EC-01 bath: filtration bags replaced and ultrafiltrate partially dumped (2,000 l) on 2024-07-10.

# D4 · Root cause analysis

Investigation on 2024-07-13–2024-07-15 with the chemistry supplier S-ARAK (Química Araxes S.A.).

Ishikawa diagram (6M)

| Category | Potential cause | Verification / status |
| --- | --- | --- |
| Material | Make-up chemistry lot S-ARAK-240132 with phosphate content above target | CONFIRMED – bath phosphate 42 ppm (target < 20 ppm) after make-up of 27/05/2024 |
| Method | DI rinse before the e-coat tank: conductivity > 30 µS/cm | CONFIRMED (contributing) – 38 µS/cm recorded on 30–31/05/2024 |
| Machine | Filtration bags overdue (changed every 2 weeks, last change 12 days before) | Contributing |
| Man | Bath titration by night-shift operator | Ruled out – titrations performed per plan |
| Measurement | Final inspection checks thickness only, no pore check | CONFIRMED (non-detection) |
| Environment | Oven HC-01 curing profile | Ruled out – 180 °C / 20 min verified with data logger |

5 Whys — occurrence

| Why |  |
| --- | --- |
| 1 | Why pores/craters? — Contaminant particles and phosphate carry-over in the e-coat bath. |
| 2 | Why contamination? — Bath make-up with chemistry lot S-ARAK-240132 raised phosphate to 42 ppm, and the DI rinse was above 30 µS/cm. |
| 3 | Why was the chemistry lot accepted? — Incoming inspection of chemistry relied on the supplier certificate only. |
| 4 | Why was the high rinse conductivity not acted on? — No alarm limit on the DI rinse; the value was logged but not reviewed on the night shift. |

5 Whys — non-detection

| Why |  |
| --- | --- |
| 1 | Why was the defect not detected at Arga? — Final inspection (VI-01) checks thickness on 1 part in 20; no porosity or salt spray test in series. |

Root cause — occurrence: Bath contamination from chemistry lot S-ARAK-240132 (phosphate above target) combined with insufficient DI rinsing before the e-coat tank.

Root cause — non-detection: No porosity check and no periodic corrosion test in the control plan; thickness measurement alone does not detect pinholes.

Root cause verification: Lab panels coated on 2024-07-14 with contaminated bath sample → 11 craters/dm²; with fresh bath + DI rinse < 10 µS/cm → 0 craters/dm².

# D5 · Permanent corrective actions (chosen)

| Action | Type | Owner | Due date |
| --- | --- | --- | --- |
| Incoming check of each S-ARAK chemistry lot (phosphate + conductivity) before bath addition | Corrective – occurrence | Garazi Lizarraga | 2024-07-19 |
| DI rinse conductivity alarm at 20 µS/cm with line stop | Corrective – occurrence | Koldo Arbizu | 2024-07-21 |
| Filtration bag change weekly | Corrective – occurrence | Garazi Lizarraga | 2024-07-16 |
| Porosity check (visual 1,000 lux) 5 parts per rack + monthly salt spray test | Corrective – detection | Mikel Aranburu | 2024-07-23 |

# D6 · Implementation and validation

Actions effective from 2024-07-23. IT-L3-EC01-02 updated to v2 on 2024-07-29. S-ARAK issued its own 8D (supplier ref. SA-24-117) and quarantined the batch.

Validation results

Bath phosphate < 15 ppm since mid-July 2024 (daily titration).

Salt spray 480 h: 3 of 3 monthly samples without red rust.

No further OEM Norte complaints on e-coat in 90 days.

# D7 · Actions to prevent recurrence

| Action | Document / system | Owner | Due date | Status |
| --- | --- | --- | --- | --- |
| PFMEA e-coat: causes 'chemistry contamination' and 'rinse conductivity' | AMFE-L3-EC01-01 v2 | Garazi Lizarraga | 2024-08-08 | Done |
| Control plan e-coat: incoming chemistry check, rinse alarm, porosity check | PC-L3-EC01-01 v2 | Garazi Lizarraga | 2024-08-08 | Done |
| Supplier evaluation S-ARAK: quality incident recorded | Supplier evaluation 2024 | Leire Sarasola | 2024-08-23 | Done |

# D8 · Closure and team recognition

8D closed on 2024-10-01; accepted by OEM Norte SQE.

| Role | Name | Date | Signature |
| --- | --- | --- | --- |
| Customer Quality Engineer (8D leader) | Maialen Irigoyen | 2024-10-01 | signed |
| Quality Manager (champion) | Iñaki Etxeberria | 2024-10-01 | signed |
| OEM Norte SQE (acceptance) | M. Ruiz | 2024-10-04 | accepted |