8D REPORT — OEM Norte Supplier Quality

Form OEMN-SQ-8D rev. 3 · to be returned within 10 working days

| Supplier | Componentes Arga S.L. | Supplier code | ARGA |
| --- | --- | --- | --- |
| OEM Norte complaint no. | C-OEMN-2024-0191 | Supplier 8D no. | 8D-ARGA-2024-013 |
| Part number | AR-1006 | Part description | A/C compressor bracket |
| Special characteristic | Weld nut torque (SC) | Supplier lot | L24295-AR1006-01 |
| Complaint date | 2024-12-03 | Qty complained | 75 |
| Containment due (24 h) | 2024-12-04 | 8D due (10 WD) | 2024-12-17 |
| Report status | CLOSED | Closure date | 2025-02-13 |

# D1 · Team

| Name | Role | Department |
| --- | --- | --- |
| Iñaki Etxeberria | Quality Manager (champion) | Quality |
| Maialen Irigoyen | Customer Quality Engineer (8D leader) | Quality |
| Oihana Zabaleta | Welding Process Engineer | Engineering L2 |
| Koldo Arbizu | Maintenance Manager | Maintenance |
| Xabier Urrutia | Production Manager L2 | Production |
| Mikel Aranburu | Metrology & Lab Technician | Quality |

Customer contact: M. Ruiz, Supplier Quality Engineer, OEM Norte.

# D2 · Problem description (5W2H)

Problem statement

OEM Norte reported 75 A/C compressor brackets (AR-1006) whose M8 weld nut detached or turned below the torque-out requirement (≥ 40 Nm) when tightening the compressor bolts. Lot L24295-AR1006-01.

| 5W2H |  |
| --- | --- |
| What | Weld nut M8 torque-out 12–30 Nm (spec ≥ 40 Nm); 1 or 2 of the 3 projections not fused. |
| Where | OEM Norte front-end module line. Origin: Arga L2, projection welding with SP-01 and nut feeder AT-01. |
| When | Lot produced 21/10/2024 (night shift), delivered 26–27/10/2024, detected 02/12/2024. |
| Who | OEM Norte assembly operator (nut spinning with the DC nutrunner). |
| Which | AR-1006 only. |
| How | Off-centre weld: projections on one side not fused, witness marks show nut offset 0.8 mm. |
| How many | 75 NOK out of 2,965 delivered. |

Lot L24295-AR1006-01: produced 2024-10-21 (night shift), press PR-250, cell SP-01, 3,000 parts produced, 35 scrapped. Steel coil S-ULTZ-240144, weld nuts S-BIDA-240140, e-coat chemistry S-ARAK-240144.

# D3 · Interim containment actions

Containment started on 2024-12-03. Scope: AR-1006 lots welded on SP-01 from the complained lot up to notification.

| Lot | Part | Prod. date | Shift | Qty OK produced | Shipped (delivery notes) | Arga stock | Action | Result |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| L24295-AR1006-01 | AR-1006 | 2024-10-21 | night | 2,965 | 2,965 (AL-24-00634, AL-24-00633) | 0 | Sorting at customer | 81 NOK |
| L24302-AR1006-01 | AR-1006 | 2024-10-28 | morning | 991 | 991 (AL-24-00651) | 0 | Sorting at customer | 6 NOK |
| L24309-AR1006-01 | AR-1006 | 2024-11-04 | afternoon | 2,256 | 2,256 (AL-24-00667, AL-24-00668) | 0 | Sorting at customer | 0 NOK |
| L24316-AR1006-01 | AR-1006 | 2024-11-11 | night | 2,469 | 2,469 (AL-24-00682) | 0 | Sorting at customer | 0 NOK |
| L24323-AR1006-01 | AR-1006 | 2024-11-18 | morning | 1,691 | 1,691 (AL-24-00697) | 0 | Sorting at customer | 0 NOK |
| L24330-AR1006-01 | AR-1006 | 2024-11-25 | afternoon | 1,295 | 1,295 (AL-24-00711) | 0 | Sorting at customer | 0 NOK |
| L24337-AR1006-01 | AR-1006 | 2024-12-02 | night | 2,948 | 0 | 2,948 | Blocked + 100 % sorting | 0 NOK |

Arga stock (2,948 parts) blocked on 2024-12-03; torque-out test on 5 parts per box, 100 % sorting of boxes with any NOK.

OEM Norte stock sorted by Arga on 2024-12-04–2024-12-05 with a torque wrench at 40 Nm (non-destructive proof torque).

# D4 · Root cause analysis

Root cause workshop on 2024-12-07 with maintenance and welding engineering.

Ishikawa diagram (6M)

| Category | Potential cause | Verification / status |
| --- | --- | --- |
| Machine | Upper electrode of SP-01 misaligned after replacement of the lower electrode insulating sleeve on 18/10/2024 | CONFIRMED – offset 0.8 mm measured |
| Method | No first-part torque test after maintenance on SP-01 | CONFIRMED |
| Material | Weld nut lot S-BIDA-240140 (M8 Zn-Ni) | Ruled out – coating thickness 9–10 µm, projection height conform |
| Man | Operator loading nuts manually when AT-01 jams | Ruled out – no jams recorded on 21/10/2024 |
| Measurement | Torque-out test only 1 part at start of shift | CONFIRMED (non-detection) |
| Environment | Cooling water temperature of SP-01 | Ruled out |

5 Whys — occurrence

| Why |  |
| --- | --- |
| 1 | Why low torque-out? — Only 1–2 of 3 projections fused. |
| 2 | Why? — The nut was welded off-centre (0.8 mm) relative to the electrode. |
| 3 | Why? — The upper electrode was misaligned after the lower electrode sleeve was replaced on 18/10/2024. |
| 4 | Why was it not corrected? — Maintenance released the machine without an alignment check or a torque test on the first part. |

5 Whys — non-detection

| Why |  |
| --- | --- |
| 1 | Why not detected? — Torque-out test was performed only once per shift, at the start; the night shift of 21/10/2024 started before the maintenance was completed. |

Root cause — occurrence: Electrode misalignment on SP-01 after maintenance, causing off-centre projection welds.

Root cause — non-detection: No release test after maintenance and insufficient torque-out test frequency.

Root cause verification: Trial on 2024-12-08: 0.8 mm offset → 7/10 parts below 40 Nm; aligned electrode → 10/10 above 62 Nm.

# D5 · Permanent corrective actions (chosen)

| Action | Type | Owner | Due date |
| --- | --- | --- | --- |
| Electrode alignment gauge and check after every electrode intervention | Corrective – occurrence | Koldo Arbizu | 2024-12-13 |
| First-part torque test mandatory for machine release after maintenance | Corrective – occurrence | Oihana Zabaleta | 2024-12-13 |
| Torque-out test 3 parts every 2 h | Corrective – detection | Xabier Urrutia | 2024-12-10 |

# D6 · Implementation and validation

All actions implemented by 2024-12-17. IT-L2-SP01-02 updated (v3) with the alignment check and release test.

Validation results

Torque-out ≥ 55 Nm in all checks during 8 weeks.

No recurrence at OEM Norte in 90 days.

# D7 · Actions to prevent recurrence

| Action | Document / system | Owner | Due date | Status |
| --- | --- | --- | --- | --- |
| PFMEA SP-01: cause 'electrode misalignment after maintenance' | AMFE-AR1006-01 v2 | Oihana Zabaleta | 2025-01-07 | Done |
| Control plan: torque-out every 2 h | PC-AR1006-01 v2 | Maialen Irigoyen | 2025-01-07 | Done |
| Maintenance release checklist for all welding equipment | Maintenance system | Koldo Arbizu | 2025-01-17 | Done |

# D8 · Closure and team recognition

8D closed on 2025-02-13; accepted by OEM Norte.

| Role | Name | Date | Signature |
| --- | --- | --- | --- |
| Customer Quality Engineer (8D leader) | Maialen Irigoyen | 2025-02-13 | signed |
| Quality Manager (champion) | Iñaki Etxeberria | 2025-02-13 | signed |
| OEM Norte SQE (acceptance) | M. Ruiz | 2025-02-16 | accepted |