8D REPORT — OEM Norte Supplier Quality

Form OEMN-SQ-8D rev. 3 · to be returned within 10 working days

| Supplier | Componentes Arga S.L. | Supplier code | ARGA |
| --- | --- | --- | --- |
| OEM Norte complaint no. | C-OEMN-2025-0156 | Supplier 8D no. | 8D-ARGA-2025-008 |
| Part number | AR-1010 | Part description | Power inverter bracket |
| Special characteristic | Weld nut torque (SC) | Supplier lot | L25129-AR1010-01 |
| Complaint date | 2025-06-17 | Qty complained | 48 |
| Containment due (24 h) | 2025-06-18 | 8D due (10 WD) | 2025-07-01 |
| Report status | CLOSED | Closure date | 2025-09-05 |

# D1 · Team

| Name | Role | Department |
| --- | --- | --- |
| Iñaki Etxeberria | Quality Manager (champion) | Quality |
| Maialen Irigoyen | Customer Quality Engineer (8D leader) | Quality |
| Oihana Zabaleta | Welding Process Engineer | Engineering L2 |
| Leire Sarasola | Supplier Quality Engineer | Purchasing |
| Mikel Aranburu | Metrology & Lab Technician | Quality |
| Xabier Urrutia | Production Manager L2 | Production |

Customer contact: M. Ruiz, Supplier Quality Engineer, OEM Norte.

# D2 · Problem description (5W2H)

Problem statement

OEM Norte reported 48 power inverter brackets (AR-1010) whose M8 weld nut spins when tightening the inverter fixing bolt (torque 25 Nm). Lot L25129-AR1010-01.

| 5W2H |  |
| --- | --- |
| What | Weld nut rotates at 18–30 Nm (torque-out requirement ≥ 40 Nm); cold projection welds. |
| Where | OEM Norte e-drive module line. Origin: Arga L2, projection nut welding station of cell CR-02 (feeder AT-01). |
| When | Lot produced 09/05/2025 (morning shift), delivered 14 and 16/05/2025, detected 16/06/2025. |
| Who | OEM Norte assembly operator. |
| Which | Parts welded with weld nut lot S-BIDA-250129. |
| How | Projections flattened but not fused; bright zinc-nickel residue in the weld interface. |
| How many | 48 NOK out of 1,886 delivered. |

Lot L25129-AR1010-01: produced 2025-05-09 (morning shift), press PR-400, cell CR-02, 1,900 parts produced, 14 scrapped. Steel coil S-ULTZ-250173, MIG wire S-GOIE-250124, weld nuts S-BIDA-250129, e-coat chemistry S-ARAK-250132.

# D3 · Interim containment actions

Containment started on 2025-06-17, within 24 h. Scope: AR-1010 lots from the complained lot until the notification date.

| Lot | Part | Prod. date | Shift | Qty OK produced | Shipped (delivery notes) | Arga stock | Action | Result |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| L25129-AR1010-01 | AR-1010 | 2025-05-09 | morning | 1,886 | 1,886 (AL-25-00303, AL-25-00302) | 0 | Sorting at customer | 52 NOK |
| L25136-AR1010-01 | AR-1010 | 2025-05-16 | afternoon | 1,893 | 1,893 (AL-25-00316, AL-25-00317) | 0 | Sorting at customer | 9 NOK |
| L25143-AR1010-01 | AR-1010 | 2025-05-23 | night | 2,761 | 2,761 (AL-25-00331, AL-25-00332) | 0 | Sorting at customer | 0 NOK |
| L25150-AR1010-01 | AR-1010 | 2025-05-30 | morning | 1,773 | 1,773 (AL-25-00346) | 0 | Sorting at customer | 0 NOK |
| L25157-AR1010-01 | AR-1010 | 2025-06-06 | afternoon | 2,562 | 2,562 (AL-25-00361) | 0 | Sorting at customer | 0 NOK |
| L25164-AR1010-01 | AR-1010 | 2025-06-13 | night | 2,767 | 1,383 (AL-25-00374) | 1,384 | Blocked + 100 % sorting | 0 NOK |

Arga stock (1,384 parts) blocked on 2025-06-17; proof torque 40 Nm on 100 % of parts with nut lot S-BIDA-250129.

OEM Norte stock sorted on 2025-06-18–2025-06-19 by the Arga resident team (proof torque 40 Nm).

Remaining nuts of lot S-BIDA-250129 quarantined and returned to the supplier on 2025-06-20.

# D4 · Root cause analysis

Investigation on 2025-06-21–2025-06-23 with the nut supplier S-BIDA (Fijaciones Bidasoa S.L.).

Ishikawa diagram (6M)

| Category | Potential cause | Verification / status |
| --- | --- | --- |
| Material | Zn-Ni coating thickness of nut lot S-BIDA-250129 at the upper limit (11.5–12.0 µm, spec 8–12 µm) | CONFIRMED – noted at incoming inspection |
| Method | Weld schedule validated only with mid-range coating (9–10 µm) | CONFIRMED |
| Machine | Electrode wear / alignment of the nut station | Ruled out – within limits |
| Man | — | Not related |
| Measurement | Torque-out test 1 part per shift | CONFIRMED (non-detection) |
| Environment | — | Not related |

5 Whys — occurrence

| Why |  |
| --- | --- |
| 1 | Why does the nut spin? — The projections are not fused. |
| 2 | Why? — Energy at the interface was insufficient: the thicker Zn-Ni coating increases contact resistance and zinc vapour. |
| 3 | Why was energy insufficient? — The weld schedule was validated only with coating in the middle of the range. |
| 4 | Why was the lot used? — Coating was within specification; no rule to adjust or segregate lots at the limit. |

5 Whys — non-detection

| Why |  |
| --- | --- |
| 1 | Why not detected? — Torque-out test was performed only once per shift. |

Root cause — occurrence: Weld nuts with Zn-Ni coating at the upper tolerance combined with a weld schedule not validated for that condition.

Root cause — non-detection: Insufficient torque-out test frequency.

Root cause verification: Trial on 2025-06-23: nuts with 11.8 µm coating → 6/10 below 40 Nm; with +8 % weld current → 10/10 ≥ 58 Nm; nuts with 9.5 µm → 10/10 ≥ 60 Nm.

# D5 · Permanent corrective actions (chosen)

| Action | Type | Owner | Due date |
| --- | --- | --- | --- |
| S-BIDA: coating window for Arga restricted to 8–11 µm (drawing note + PCN) | Corrective – occurrence | Leire Sarasola | 2025-07-17 |
| Incoming XRF coating measurement per nut lot | Corrective – occurrence | Mikel Aranburu | 2025-07-01 |
| Weld schedule revalidated across the full coating range | Corrective – occurrence | Oihana Zabaleta | 2025-07-08 |
| Torque-out 3 parts every 2 h | Corrective – detection | Xabier Urrutia | 2025-06-24 |

# D6 · Implementation and validation

Implemented by 2025-07-17. S-BIDA confirmed the restricted window from its lot of July 2025.

Validation results

Torque-out ≥ 52 Nm in all checks over 10 weeks.

No recurrence at OEM Norte in 90 days.

# D7 · Actions to prevent recurrence

| Action | Document / system | Owner | Due date | Status |
| --- | --- | --- | --- | --- |
| PFMEA nut welding: cause 'coating at upper limit' | AMFE-AR1006-01 v3 (AR-1006/AR-1010) | Oihana Zabaleta | 2025-07-22 | Done |
| Control plan: XRF at incoming + torque-out every 2 h | PC-AR1006-01 v3 | Maialen Irigoyen | 2025-07-22 | Done |
| Read-across to AR-1006 on SP-01 | IT-L2-SP01-02 v4 | Oihana Zabaleta | 2025-07-27 | Done |

# D8 · Closure and team recognition

8D closed on 2025-09-05; accepted by OEM Norte.

| Role | Name | Date | Signature |
| --- | --- | --- | --- |
| Customer Quality Engineer (8D leader) | Maialen Irigoyen | 2025-09-05 | signed |
| Quality Manager (champion) | Iñaki Etxeberria | 2025-09-05 | signed |
| OEM Norte SQE (acceptance) | M. Ruiz | 2025-09-08 | accepted |